USEFUL DESIGN PARAMETERS (simplified)

0.18m			0.13m

Name				Symbol	NMOS	PMOS	NMOS	PMOS	Units

Channel Length		L		200nm	200nm	100nm	100nm	nm

(rounded for convenience)

Supply Voltage		VDD		1.8		1.8		1.2		1.2	           V

Oxide Thickness		tox		35		35		22		22		Å

Oxide Capacitance	Cox		1.0 		1.0		1.6		1.6 	       F/cm2

Threshold Voltage	VTO		0.5		-0.5		0.4		-0.4              V

Body-effect term				0.3		0.3		0.2		0.2                V1/2

Fermi Potential		2|F|		0.84		0.84		0.88		0.88		  V

Junction Capacitance	Cjo		1.6		1.6		1.6		1.6	       fF/m2

Coefficient

Built-in Junction		B		0.9		0.9		1.0		1.0		  V

Potential

Grading Coefficient	m		0.5		0.5		0.5		0.5		  -

Nominal Mobility	o		540		180		540		180	      cm2/V-s

(low vertical field)

Effective Mobility 	e		270		70		270		70	      cm2/V-s

(high vertical field)

Critical Field		Ec		6 x 104	24 x 104	6 x 104	24 x 104    V/cm

Critical Field x L		EcL		1.2		4.8		0.6		2.4		 V

Effective Resistance	Reff		12.5	 	30		12.5		30		k/ڤ

Name						Symbol		Value		Units

Gate Capacitance Coefficient		Cg 			2		fF/m

Self Capacitance Coefficient		Ceff			1		fF/m

Wire Capacitance Coefficient		Cw			0.1-0.25	fF/m

Al Wire Resistance 			Rڤ			25-60		m/ڤ

Cu Wire Resistance 			Rڤ			20-40		m/ڤ

Wire Inductance				Leff			40-50		pH/m

USEFUL PHYSICAL AND MATERIAL CONSTANTS

Name						Symbol		Value			Units

Electron Charge				q			1.6 x 10-19		C

Boltzmann’s Constant			k			1.38 x 10-23		J/oK

Room Temperature			T			300			oK (27oC)

Thermal Voltage				Vth=kT/q		26			mV (at 27oC)

Dielectric Constant of Vacuum				8.85 x 10-14		F/cm

Dielectric Constant of Silicon					11.7		F/cm

Dielectric Constant of SiO2					3.97		F/cm

Intrinsic Carrier Concentration	ni			1.45 x 1010		/cm3 (at 27oC)

Carrier Saturation Velocity		sat 			8 x 106		cm/s

In Silicon

Aluminum Resistivity   					2.7			cm

Copper Resistivity        						1.7			cm

Tungsten Resistivity						5.5			cm

ENGINEERING SCALE FACTORS

G	giga		109

M	mega		106

k	kilo		103

c	centi		10-2

m	milli		10-3

	micro		10-6

n	nano		10-9

p	pico		10-12

f	femto		10-15

a	atto		10-18

METER CONVERSION FACTORS

1m = 10-4 cm = 10-6 m

1 m = 102 cm = 106 m

0.1 m = 100 nm

1Å = 10-8cm = 10-10m